Investigation of the decomposition products and kinetics of degradation of ZIF-8 in lactic acid

Butonova S. А., E. V. Ikonnikova, A. V. Vinogradov

Master student, 2 year

ITMO University, Saint Petersburg, Russia

E–mail: butonova@scamt-itmo.ru

Metal-organic frameworks (MOFs) are one of the most attractive carriers for targeted drug delivery. Due to their flexible structure with a combination of unique properties such as crystallinity, porosity, and the presence of strong metal-ligand interactions, they provide a good outlook for targeted drug delivery [1].

Among MOFs, ZIF-8 which consists of (Zn(mim)2, mim = 2-methylimidazolate) is considered one of the most promising substances for drug delivery systems due to their ability to degrade in acidic media [1]. The extracellular environment in a tumor is more acidic than in normal tissues because of a “Warburg effect”. A large amount of lactate secreted by the tumor cells [2]. Therefore, we chose lactic acid as the substance that acidified ZIF-8 particles. However, ZIF-8 can be degraded not only in the presence of lactate but also in the presence of various ions [3]. In this work, we concentrated on phosphorus ions because they are included in PBS, which is a buffer solution for studying the release kinetics of encapsulated molecules in MOFs [1]. The comparison of Hmim release in PBS solution and NaCl (reference solution) will lead us to a better understanding of what is influenced on the decomposition rate of ZIF-8 to a greater extent: the influence of phosphate groups or pH of the solutions.

Moreover, for considering ZIF-8 in biomedical applications especially in drug delivery, for future application and for the transition from in vitro to in vivo experiments, a compound must be biocompatible. To make sure that the drug@ZIF-8 system can be used for targeting drug delivery, it is necessary to evaluate the toxicity of the decomposition products [4]. Thus, the second goal of this research is to investigate the influence of these products on normal cells.

Figure 1. – Scheme of degradation ZIF-8 in PBS and NaCl solutions.

Acknowledgements

This work was supported by the Russian Science Foundation (Grant No. 19-19-00433).

References

1.	Sharsheeva A. et al. Light-controllable systems based on TiO2-ZIF-8 composites for targeted drug release: Communicating with tumour cells // J. Mater. Chem. B. Royal Society of Chemistry, 2019. Vol. 7, № 43. P. 6810–6821.

2.	Annibaldi A., Widmann C. Glucose metabolism in cancer cells // Curr. Opin. Clin. Nutr. Metab. Care. 2010. Vol. 13, № 4. P. 466–470.

3.	Wang H. et al. Specific anion effects on the stability of zeolitic imidazolate framework-8 in aqueous solution // Microporous Mesoporous Mater. 2018. Vol. 259, № August 2017. P. 171–177.

4.	Simon-Yarza T. et al. Nanoparticles of Metal-Organic Frameworks: On the Road to In Vivo Efficacy in Biomedicine // Adv. Mater. 2018. Vol. 30, № 37. P. 1–15.