Описание структуры икосаэдрических квазикристаллов

Мадисон П.А.

Аспирант, 2 год обучения

Санкт-Петербургский государственный электротехнический университет «ЛЭТИ» им. В.И. Ульянова (Ленина), факультет электроники, Санкт-Петербург, Россия

E-mail: palmadis@mail.ru

Описание структуры икосаэдрических квазикристаллов – важная задача современного материаловедения. На сегодняшний день для этих целей обычно используется многомерная кристаллография. В рамках такого подхода структура икосаэдрических квазикристаллов получается в результате проецирования 3D-среза из шестимерного пространства в трехмерное.

Нами разрабатывается альтернативный подход, основанный на использовании нескольких квази-элементарных ячеек. Результаты изложены в работах [1,2]. Наш метод базируется на использовании разбиения Соколара-Стейнхардта [3] с четырьмя типами «золотых» зоноэдров (ромбический триаконтаэдр, ромбический икосаэдр, ромбический додэкаэдр и вытянутый ромбоэдр). Заполнение пространства зоноэдрами осуществляется при помощи итерационного алгоритма на основе оригинальных правил подстановок [4,5]. Заполнение квази-элементарных ячеек атомами подчиняется строгим правилам [2].

Развиваемый нами подход показал высокую эффективность и хорошо зарекомендовал себя при моделировании свойств квазикристаллов [6,7].

Литература

1. Madison A.E., Madison P.A. Looking for Alternatives to the Superspace Description of Icosahedral Quasicrystals // Proceedings of the Royal Society A: Mathematical, Physical and Engineering Sciences. 2019, №475(2221), 20180667.

2. Madison A.E., Madison P.A. Structure of Icosahedral Quasicrystals within the 
Multiple-cell Approach // Structural Chemistry. 2020, №31(1). p. 1–21.

3. Socolar J.E.S., Steinhardt P.J. Quasicrystals. II. Unit-cell configurations // Physical Review B. 1986, №34(2). p. 617–647.

4. Madison A.E. Substitution Rules for Icosahedral Quasicrystals. // RSC Advances. 2015, №5(8). p. 5745-5753.

5. Madison A.E. Atomic Structure of Icosahedral Quasicrystals: Stacking Multiple 
Quasi-unit Cells. // RSC Advances. 2015, №5(97). p. 79279-79297.

6. Jeon S.Y., Kwon H., Hur K. Intrinsic Photonic Wave Localization in a Three-dimensional Icosahedral Quasicrystal // Nature Physics. 2017, №13(4). p. 363-368.

7. Casas L. Teaching Periodicity and Aperiodicity Using 3D-printed Tiles and Polyhedra // Journal of Applied Crystallography. 2020, №53(6). p. 1583-1592.