Моделирование и разработка селекторных приборов для матриц резистивной памяти

Федотов М.И.1

Студент

Коротицкий В.И.2

Старший инженер

Ковешников С.В.2

Заместитель директора по инновациям, кандидат физико-математических наук

1Московский физико-технический институт (научно-исследовательский университет), физтех-школа электроники, фотоники и молекулярной физики, г. Долгопрудный, Россия

mf98orion@gmail.com

2Институт проблем технологии микроэлектроники и особо чистых материалов РАН

Черноголовка, Россия

skoveshnikov@iptm.ru

Резистивная память (ReRAM) является многообещающим кандидатом для перспективной энергонезависимой памяти благодаря своей масштабируемости, высокой скорости чтения и записи, низкому энергопотреблению и простоте [1], [2]. Тем не менее, с постоянно уменьшающимися размерами устройств наноэлектроники возникают проблемы, связанные с токами утечки и сопротивлением межсоединений [3], [4]. В структурах Crossbar эти проблемы ограничивают максимальный размер массива памяти, поскольку матрицы энергонезависимой резистивной памяти большого объема с архитектурой Crossbar требуют наличия селекторных устройств с нелинейными вольтамперными характеристиками для решения проблемы паразитных токов утечки.  Существует множество способов реализации таких устройств [5]-[20], но несмотря на некоторый прогресс, остаются нерешенными проблемы создания матриц резистивной памяти с высокой плотностью записи, а также создания селектора с высокой нелинейностью, высокой плотностью тока и быстрой скоростью переключения [21].

Предлагаемое нами решение заключается в создании самосовмещенных с ячейкой памяти селекторов на основе туннельного MIM-диода, где площадь селектора совпадает с площадью самой ячейки памяти. Выбор такого варианта селектора обусловлен тем, что из всех возможных вариантов именно самосовмещенный селектор обладает наименьшей возможной площадью, и следовательно – позволяет делать массивы памяти с большой плотностью записи, а MIM-структура обеспечивает требуемую степень нелинейности вольт-амперной характеристики. Иные варианты, к примеру – применение транзисторов, требует дополнительного питания и места на кристалле. Подобные разработки ведутся в других исследовательских группах [7], [9], [11], [12], однако упор делается на эмпирические исследования, что является малоэффективным. Наш подход заключается в предварительных теоретических расчетах диодных характеристик однослойных и многослойных диэлектрических пленок в зависимости от их толщины, ширины запрещенной зоны и диэлектрической проницаемости с последующей экспериментальной апробацией. Были проведены расчеты вольт-амперных характеристик для десятков различных сочетаний материалов диэлектрика и электродов, из которых выбраны наиболее оптимальные варианты для создания самосовмещенных селекторов для существующих мемристоров на основе оксида гафния.

Литература

[1] R. Waser, M. Aono Nanoionics-based resistive switching memories // Nat. Mater., vol. 6, no. 11, pp. 833–840. Nov. 2007.

[2] J. J. Yang, D. B. Strukov, D. R. Stewart Memristive devices for computing // Nat. Nanotechnol., vol. 8, no. 1, pp. 13–24, Dec. 2012.

[3] International Technology Roadmap for Semiconductors // Denver, CO, USA, ITRS, 2012.

[4] A. Flocke and T. G. Noll Fundamental analysis of resistive nanocrossbars for the use in hybrid nano/CMOS-memory // Proc. 33rd ESSCIRC, Sep. 2007, pp. 328–331.

[5] M.-J. Lee et al. Low-temperature-grown transition metal oxide based storage materials and oxide transistors for high-density non-volatile memory // Adv. Funct. Mater., vol. 19, no. 10, pp. 1587–1593, Dec. 2008.

[6] K.-H. Kim, S. H. Jo, S. Gaba, and W. Lu  Nanoscale resistive memory with intrinsic diode characteristics and long endurance // Appl. Phys. Lett., vol. 96, no. 5, pp. 053106–053108, Feb. 2010.

[7] J.-J. Huang, Y.-M. Tseng, C.-W. Hsu, and T.-H. Hou Bipolar nonlinear Ni/TiO2/Ni selector for 1S1R crossbar array applications // IEEE Electron Device Lett., vol. 32, no. 10, pp. 1427–1429, Oct. 2011.

[8] A. Kawahara et al. An 8 Mb multilayered cross-point ReRAM macro with 443 MB/s write throughput // IEEE ISSCC Tech. Dig. Papers, Mar. 2012, pp. 432–434.

[9] W. Lee et al Varistor-type bidirectional switch (JMAX>107A/cm2, selectivity 104) for 3D bipolar resistive memory arrays // Proc. VLSI Symp., 2012, pp. 37–38.

[10] M.-J. Lee et al. Two series oxide resistors applicable to high speed and high density nonvolatile memory // Adv. Mater., vol. 19, no. 22, pp. 3919–3923, Nov. 2007.

[11] X. Liu et al. Diode-less bilayer oxide (WOx -NbOx ) device for crosspoint resistive memory applications // Nanotechnology, vol. 22, no. 47, pp. 475702-1–475702-3, 2011.

[12] E. Cha et al. Nanoscale (10nm) 3D vertical ReRAM and NbO2 threshold selector with TiN electrode // IEDM Tech. Dig., 2013, pp. 10.5.1–10.5.4.

[13] S. C. Puthentheradam, D. K. Schroder, and M. N. Kozicki Inherent diode isolation in programmable metallization cell resistive memory elements // Appl. Phys. A Mater. Sci., vol. 102, no. 4, pp. 817–826, Mar. 2011.

[14] K. Gopalakrishnan et al. Highly-scalable novel access device based on mixed ionic conduction (MIEC) materials for high density phase change memory (PCM) array // Proc. VLSIT, 2010, pp. 205–206.

[15] G. Burr et al. Large-scale (512 kbit) integration of multilayer-ready access-devices based on mixed-ionic-electronicconduction (MIEC) at 100% yield // VLSI Symp. Tech. Dig., Jun. 2012, pp. 41–42.

[16] V. S. S. Srinivasan et al. Punchthrough-diode-based bipolar RRAM selector by Si epitaxy // IEEE Electron Device Lett., vol. 33, no. 10, pp. 1396–1398, Oct. 2012.

[17] E. Linn, R. Rosezin, C. Kügeler, and R. Waser Complementary resistive switches for passive nanocrossbar memories // Nat. Mater., vol. 9, no. 5, pp. 403–406, May 2010.

[18] F. Nardi, S. Balatti, S. Larentis, and D. Ielmini Complementary switching in metal oxides: Toward diode-less crossbar RRAMs, // IEDM Tech. Dig., 2011, pp. 31.1.1–31.1.4.

[19] Y. Yang, P. Sheridan, and W. Lu Complementary resistive switching in tantalum oxide-based resistive memory devices // Appl. Phys. Lett., vol. 100, no. 20, pp. 203112–203115, May 2012.

[20] W. Kwon, J. Jeon, L. Hutin, and T.-J. K. Liu Electromechanical diode cell for cross-point nonvolatile memory arrays // IEEE Electron Device Lett., vol. 33, no. 2, pp. 131–133, Feb. 2012.

[21] S. Kim, J. Zhou and W. D. Lu Crossbar RRAM Arrays: Selector Device Requirements During Write Operation // IEEE Transactions on Electron Devices, vol. 61, no. 8, pp. 2820-2826, Aug. 2014, doi: 10.1109/TED.2014.2327514.